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Abstract
A series of heterogenous catalysts based on supported ruthenium were prepared from RuCl3 precusor by impregnation method. The effect of support materials (bentonite, TiO2, Al2O3 and SiO2) on catalytic activity of Ru catalyst for hydrogenolysis of glycerol were investigated under mild reaction condition of 150C and 20 bar initial hydrogen pressure for 7 hours reaction time and glycerol concentration was 20%(wt). It was found that the type of support material have significant effects on the activity and selectivity of glycerol hydrogenolysis. The order of Ru catalyst activity was Ru/bentonite > Ru/Al2O3  Ru/TiO2 > Ru/SiO2. This study showed that bentonite supported Ru catalyst was the most active with glycerol conversion reaching 62.5% compared to other supports. All the tested catalyst exhibited high selectivity to 1,2-propanediol with more than 80%. Characterization of the catalysts was carried out using BET, XPS, FESEM-EDX and TEM to obtain the physicochemical properties of the catalysts.
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Abstrak
Satu siri pemangkin heterogen berasaskan logam ruthenium berpenyokong disediakan daripada prekusor garam RuCl3 menggunakan teknik impregnasi. Kesan bahan penyokong (bentonit, TiO2, Al2O3 dan SiO2) terhadap aktiviti pemangkin Ru dalam hidrogenolisis gliserol dilakukan pada keadaan tindak balas yang sederhana dengan suhu 150C, tekanan awal hydrogen 20 bar, masa tindak balas 7 jam dan kepekatan gliserol 20%(wt). Keputusan yang diperolehi menunjukkan jenis bahan penyokong mempunyai kesan signifikan terhadap aktiviti dan pemilihan dalam hidrogenolisi gliserol. Turutan aktiviti pemangkin Ru adalah Ru/bentonit > Ru/Al2O3  Ru/TiO2 > Ru/SiO2. Kajian ini menunjukkan pemangkin Ru yang disokong atas bentonit adalah pemangkin yang paling aktif dengan peratus penukaran mencapai 62.5% berbanding dengan penyokong lain. Semua pemangkin yang diuji menunjukkan peratus pemilihan terhadap produk 1,2-propandiol yang tinggi iaitu melebihi 80%. Pencirian pemangkin dilakukan menggunakan alat BET, XPS, FESEM-EDX dan TEM bagi mendapatkan sifat-sifat fizikokimia pemangkin.
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