Malaysian Journal of Analytical Sciences Vol 20 No 6 (2016): 1359 - 1364

INTERCALATION STUDY OF CURCUMIN INTO ZINC LAYERED HYDROXIDE

(Kajian Mengenai Penyisipan Kurkumin ke dalam Zink Hidroksida Berlapis)

Adila Mohamad Jaafar1*, Asma Najaj Anuar1, Norhayati Hashim2, Fatin Hanifah Ayob1

1Department of Chemistry, Faculty of Science,

Universiti Putra Malaysia, 43400 UPM Serdang, Selangor, Malaysia

2Department of Chemistry, Faculty of Science and Mathematics

Universiti Pendidikan Sultan Idris, 35900 Tanjong Malim, Perak, Malaysia

*Corresponding author: adilamj@upm.edu.my

Received: 17 August 2015; Accepted: 5 October 2016

Abstract

Zinc layered hydroxide (ZLH) intercalated with curcumin was successfully prepared by ion exchange method. The synthesised nanocomposite was characterised by Powder X-ray diffraction (PXRD) and Fourier transform infrared spectroscopy (FTIR). The obtained intercalation compound, ZLH-curcumin nanocomposite (ZiCUR), showed a basal spacing of 10.0 Å when 0.01M of curcumin solution was used in the synthesis. The shifting in the stretching frequency of the curcumin anion provides strong evidence that the anion is bonded to the ZLH through electrostatic force. In FTIR, after intercalation, there is a noticeable shift of the O-H stretching vibrational bands. This is due to the formation of strong hydrogen bonds between curcumin and –OH groups in ZLH. Thus, this indicates that curcumin anions are present in the sample and were intercalated between positively charged ZLH layers, as indicated by the characteristics of PXRD pattern.

Keywords:  zinc layered hydroxide, curcumin, ion exchange method

Abstrak

Zink hidroksida berlapis (ZHB) disisip bersama kurkumin telah berjaya disediakan menggunakan kaedah pertukaran ion. Komposit nano yang telah di sintesis dicirikan menggunakan X-ray Serbuk Pembelauan dan Spektroskopi Infra Merah Transformasi Fourier. Sebatian interkalasi yang diperoleh iaitu komposit nano zink hidrosida berlapis-kurkumin, menunjukkan jarak basal sebanyak 10.0 Å apabila kepekatan 0.01M larutan kurkumin digunakan semasa proses sintesis. Perubahan pada frekuensi anion kurkumin menunjukkan bukti yang kukuh di mana anion telah dilekatkan kepada ZHB menggunakan daya elektrostatik. Melalui Spektroskopi Infra Merah Transformasi Fourier, selepas interkalasi, perubahan yang ketara pada O-H regangan jalur getaran dapat di lihat. Hal ini kerana, pembentukan ikatan hidrogen yang kuat antara kurkumin dan kumpulan -OH di dalam ZHB. Maka, ia menunjukkan bahawa anion kurkumin hadir di dalam sampel dan telah disisipkan antara lapisan ZHB yang bercas positif, seperti mana yang ditunjukkan oleh ciri – ciri corak Spektroskopi Infra Merah Transformasi Fourier.

Kata kunci:  zink hidroksida berlapis, kurkumin, kaedah pertukaran ion

References

- Wound Reach Foundation (2015). Online from http://www.woundreach.org/why-wounds/the-challenge [Accessed date 2015-06-27].

- Gadekar, R., Saurabh, M. K., Thakur, G. S. and Saurabh, A. (2012). Study of formulation, characterisation and wound healing potential of transdermal patches of curcumin. Asian Journal of Pharmaceutical and Clinical Research, 5(4): 225 – 230.

- Bharat, B., Kumar, A., Aggarwal, M. S. and Shishodia, S. (2005). Curcumin derived from turmeric (Curcuma Longa): A spice for all seasons. Phytopharmaceuticals in Cancer Chemoprevention, 23: 351 – 387.

- Kamkanam, M., Samindra, S. and Kottegoda, N. (2014). Encapsulation of curcumin into layered double hydroxides. Nanotechnology Reviews, 3(6): 579 – 589.

- Aminu, U. K., Hussein, M. Z., Fakurazi, S. and Arulselvan, P. (2014). Layered double hydroxide nanocomposite for drug delivery systems; bio-distribution, toxicity and drug activity enhancement. Chemistry Central Journal, 8: 47 – 55.

- Cao, G. T., Xing, F. F., Wang, P. and Ni, Z. M. (2008). Synthesis, characterization and release of curcumin-intercalated Mg-Al-layered double hydroxides. Chinese Journal of Inorganic Chemistry, 24(6): 956 – 963.

- Ramli, M., Hussein, M. Z. and Yusoff, K. (2013). Preparation and characterization of an anti-inflammatory agent based on a zinc-layered hydroxide-salicylate nanohybrid and its effect on viability of Vero-3 cells. International Journal of Nanomedicine, 2013 (8): 297 – 306.

- Kang, H., Leoni, M., He, H., Huang, G. and Yang, X. (2012). Well-crystallized CO32- - type LiAl-LDH from urea hydrolysis of an aqueous chloride solution. European Journal of Inorganic Chemistry, 2012(24): 3859 – 3865.

- Hussein, M. Z., Ghotbi, M. Y., Yahaya, A. H. and Rahman, M. Z. A. (2009). Synthesis and characterization of (zinc-layered-gallate) nanohybrid using structural memory effect. Materials Chemistry and Physics,113 (1): 491 – 496.

- Hussein, M. Z., Jaafar, A. M., Yahaya, A. H. and Zulkarnain, Z. (2009). The effect of single, binary and ternary anions of chloride, carbonate and phosphate on the release of 2, 4-dichlorophenoxyacetate intercalated into the Zn-Al-layered double hydroxide nanohybrid. Nanoscale Research Letters, 4 (11): 1351 – 1357.

- Rajamathi, M. and Kamath, P. V. (2001). Urea hydrolysis of cobalt(II) nitrate melts: synthesis of novel hydroxides and hydroxynitrates. International Journal of Inorganic Materials, 3 (7): 901 – 906.

- Hussein, M. Z., Rahman, N. S. S. A., Sajiro, S. H. and Zainal, Z. (2012). Herbicide-intercalated zinc layered double hydroxide nanohybrid for a dual-guest controlled release formulation. International Journal of Molecular Sciences, 13: 7328 – 7342.

- Hashim, N., Muda, Z., Hamid, S. H., Isa, I. M., Kamari, A., Mohamed, A., Hussein, M. Z. and Ghani, S. A. (2014). Characterization and controlled release formulation of agrochemical herbicides based on zinc-layered hydroxide-3-(4-methoxyphenyl) propionate  nanocomposite. Journal of Physical and Chemical Sciences, 1(4): 1 – 6.

- Hashim, N., Hussein, M. Z., Isa, I. M., Kamari, A., Mohamed, A., Jaafar, A. M. and Taha, H. (2014). Synthesis and controlled release of cloprop herbicides from cloprop-layered double hydroxide and cloprop-zinc-layered hydroxide nanocomposites. Open Journal of Inorganic Chemistry, 4: 1 – 9.

- Bang, S., Lee, S., Ko, Y., Park, J., Shin, S., Seo, H. and Jeon, H. (2012). Photocurrent detection of chemically tuned hierarchical ZnO nanostructures grown on seed layers formed by atomic layer deposition. Nanoscale Research Letters, 7: 290 – 301.

- Hussein, M. Z., Ali, S. H. A., Zainal, Z. and Hakim, M. N. (2011). Development of antiproliferative nanohybrid compound with control release property using ellagic acid as the active agent. International Journal of Nanomedicine, 6: 1373 – 1383.

- Xingfu, Z., Zhaolin, H., Yiqun, F., Su, C., Weiping, D. and Nanping, X. (2008). Microspheric organization of multilayered  ZnO  nanosheets  with hierarchically porous structures. Journal Physical Chemistry C, 112: 11722 – 11728.

- Mohsin, S. M. N., Hussein, M. Z., Sajiro, S. H., Fakurazi, S., Arulselvan, P. and Hin, T.Y.Y. (2013). Synthesis of (cinnamate-zinc layered hydroxide) intercalation compound for sunscreen application. Chemistry Central Journal, 7(1): 26 – 32.

- Lv, L., Sun, P., Gu, Z., Du, H., Pang, X., Tao, X., Xu, R. and Xu, L. (2009). Removal of chloride ion from aqueous solution by ZnAl-NO3 layered double hydroxide as anion-exchanger. Journal of Hazardous Materials, 161: 1444 – 1449.

- Hussein, M. Z., Hashim, N., Yahya, A. H. and Zainal, Z. (2010). Synthesis and characterization of [4-(2,4-dichlorophenoxybutyrate)-zinc layered hydroxide] nanohybrid. Solid State Sciences, 12: 770 – 775.